## Slide 1: Experimental and numerical assessment of the mechanics of keloid-skin composites undergoing large deformations
M. Sensale, J. Chambert, F. Chouly, A. Lejeune, S. Joly, K. Rekik,
G. Rolin, T. Lihoreau, B. Chatelain, P. Sandoz, S. Bordas, E. Jacquet

## Slide 2
Keloid scars
Goal of the project
A clinical study on a keloid specimen
Parameters identification: hyperelasticity
Modelling: image processing, CAD modelling, FEM modelling
Results & Discussion
Prospects
table of contents

## Slide 3
keloid scars (1)
“A keloid scar is defined as a dermal tumour that spreads beyond the margin of the original wound, that continues to grow over time, that does not regress spontaneously, that often recurs after excision, and has been present for at least 1 year.“ (Suarez Pozos, 2014)
Upper arm keloid (Ogawa et al., 2011)
Sternal keloid (Patel et al., 2010)
Keloid’s growth (Burd, 2008)

## Slide 4
keloid scars (2)
Crab’s clow shape keloid (Ogawa, 2008)
Butterfly shape keloid (Ogawa, 2008)
Biologic, genetic and mechanical causes
Pathogenesis still not well understood
No existing optimal treatment method
Common sites of keloid appereance (Ogawa , 2011)

## Slide 5
Develop a 3D FEM model of a real keloid starting from experimental data collected during a clinical study on a volunteer’s specimen.
Photo of the keloid’s specimen silicon molding
aim of the present study
Hypothesis: mechanical forces are responsible of keloid’s extension
Develop a method to predict keloid mechanical behaviour
Investigate the stress field in and around the keloid and directions of growth
Design a patient-specific device to prevent keloid’s growth
goal of the project

## Slide 6
Ultra-light extensiometer: uniaxial extension
Keloid specimen
A photo taken during the clinical study
a clinical study on a keloid specimen (1)

## Slide 7
Ultra-light extensiometer: uniaxial extension
A photo taken during the clinical study
a clinical study on a keloid specimen (2)
Fixed pad
Moving pad,
force sensor

## Slide 8
Ultra-light extensiometer: uniaxial extension
A photo taken during the clinical study
a clinical study on a keloid specimen (2)
U-shaped fixed guarding pad
U-shaped moving guarding pad

## Slide 9
Ultra-light extensiometer: uniaxial extension
Displacement fields following the tensile axis X and the transverse axis Y for an example with only healthy skin
a clinical study on a keloid specimen (3)

## Slide 10
Hypothesis:
constant keloid thickness
constant healthy skin thickness
uniform strain over both keloid and healthy skin
;
a clinical study on a keloid specimen (4)
Chart: Displacement (mm)

## Slide 11
Mechanical parameters identification: ANSYS® Material Curve Fitting
parameters identification: hyperelasticity(1)
Hypothesis about keloid and healthy skin materials:
Ideally elastic (no visco-elasticity)
Isotropic
Homogeneous
Incompressible
Hyperelastic (nearly incompressible )
Least squares fitting hypothesizing a uniaxial traction:
W strain density energy function
Stress

## Slide 12
Mechanical parameters identification: ANSYS® Material Curve Fitting
parameters identification: hyperelasticity(2)
Ogden 2° order (MPa) |  | 
 | Keloid | Healthy skin
μ1 | 5.07 E-06 | 9.40 E-09
α1 | 83.03 | 64.38
μ2 | 7.20 | 0.01
α2 | 0.01 | 4.90
Ogden 2nd order model
μ1, α1, μ2, α2, material constants
d1, d2 compressibility parameters
principal stretches of the deviatoric part of the deformation gradient tensor
Mooney-Rivlin 5 parameters model
c10, c01, c20, c11, c02 material constants
d compressibility parameter
I1, I2, I3 invariants of the Cauchy-Green tensor
Mooney-Rivlin 5 parameters (MPa) |  | 
 | Keloid | Healthy skin
C10 | - 0.97 | - 0.01
C01 | 0.98 | 0.02
C20 | 912.30 | 9.34
C11 | -1953.40 | - 21.36
C02 | 1048 | 12.24
, , )

## Slide 13
Alicona Infinite Focus ® : image of the silicon molding (55x20 )
image processing
3d model of a keloid scar (100x40 ) , Rhinoceros ©
CAD modelling

## Slide 14
Geometry of element SOLID187 ANSYS®
Quadratic tetrahedra
Translations x, y, z directions
Unstructured meshes
Composite keloid / healthy skin
Element SOLID187
FEM modelling (1)
An example of mesh, element size (0.9-1.1) mm

## Slide 15
Moving pads:
Fixed pads:
Dermis:
Boundary conditions
Nonlinear analysis  Newton-Raphson linearization method
FEM modelling (2)
Dirichlet boundary conditions applied on some surfaces of the model

## Slide 16
results and discussion (1)
Numerical curves fit well experimental curve up to about 3 mm
Composite model is less stiff because of the contribution of healthy skin around the keloid
Chart: Mooney-Rivlin 5 parameters
1 mm only keloid material | 0.003513 | 0.0062345 | 0.0084478 | 0.010398 | 0.012279 | 0.014223 | 0.016313 | 0.018592 | 0.021074 | 0.023753 | 0.026606 | 0.029597 | 0.032683 | 0.035817 | 0.038951 | 0.042048 | 0.045082 | 0.04805 | 0.050976 | 0.053917 | 0.056959 | 0.060212 | 0.063801 | 0.067863 | 0.072547 | 0.078013 | 0.084446 | 0.09205 | 0.10106 | 0.11175 | 0.12443 | 0.13947 | 0.1573 | 0.17839 | 0.20327 | 0.23246 | 0.26653 | 0.30601 | 0.35151 | 0.40359 | 0.46287 | 0.52997 | 0.6055 | 0.69011 | 0.78444 | 0.88914 | 1.005 | 1.1326 | 1.2725 | 1.4246
1 mm composite | 0.0037251 | 0.006743 | 0.0093092 | 0.011633 | 0.013875 | 0.01615 | 0.018536 | 0.021083 | 0.023817 | 0.026748 | 0.029864 | 0.033143 | 0.036552 | 0.040051 | 0.0436 | 0.047161 | 0.050707 | 0.054224 | 0.057719 | 0.061224 | 0.06479 | 0.068488 | 0.072406 | 0.076642 | 0.081307 | 0.08653 | 0.092458 | 0.099264 | 0.10716 | 0.11638 | 0.12723 | 0.14006 | 0.15527 | 0.17331 | 0.19463 | 0.21973 | 0.2491 | 0.28326 | 0.32278 | 0.36826 | 0.42031 | 0.47959 | 0.54676 | 0.62253 | 0.7076 | 0.80269 | 0.90848 | 1.0256 | 1.1548 | 1.2964

## Slide 17
U-shaped guarding pads boundary conditions
field without guarding pads BCs
field with guarding pads BCs
results and discussion (2)
Correlation coefficients:
All BCs  r = 0.9877
Without U pads BCs  r = 0.9729
Chart: Mooney-Rivlin 5 parameters
1mm composite: all BCs | 0.0037251 | 0.006743 | 0.0093092 | 0.011633 | 0.013875 | 0.01615 | 0.018536 | 0.021083 | 0.023817 | 0.026748 | 0.029864 | 0.033143 | 0.036552 | 0.040051 | 0.0436 | 0.047161 | 0.050707 | 0.054224 | 0.057719 | 0.061224 | 0.06479 | 0.068488 | 0.072406 | 0.076642 | 0.081307 | 0.08653 | 0.092458 | 0.099264 | 0.10716 | 0.11638 | 0.12723 | 0.14006 | 0.15527 | 0.17331 | 0.19463 | 0.21973 | 0.2491 | 0.28326 | 0.32278 | 0.36826 | 0.42031 | 0.47959 | 0.54676 | 0.62253 | 0.7076 | 0.80269 | 0.90848 | 1.0256 | 1.1548 | 1.2964
1 mm composite: without U pads BCs | 0.0095391 | 0.017973 | 0.02565 | 0.032853 | 0.039827 | 0.04677 | 0.053835 | 0.061129 | 0.06872 | 0.076641 | 0.084893 | 0.093457 | 0.10229 | 0.11136 | 0.12059 | 0.12994 | 0.13935 | 0.14878 | 0.1582 | 0.1676 | 0.17701 | 0.18648 | 0.19607 | 0.20593 | 0.21618 | 0.22703 | 0.23869 | 0.25144 | 0.26558 | 0.28145 | 0.29946 | 0.32003 | 0.34361 | 0.37069 | 0.40178 | 0.43741 | 0.47815 | 0.52458 | 0.5773 | 0.63696 | 0.7042 | 0.7797 | 0.86413 | 0.95815 | 1.0624 | 1.1776 | 1.3045 | 1.4437 | 1.5961 | 1.7621

## Slide 18
Constant keloid and healthy skin thickness
Uniform strain
Only uniaxial extension
Uncertainty quantification and sensitivity analysis about mechanical parameters in FEniCS ©
prospects (1)
Absence of experimental data about the interface keloid / healthy skin
Need data from OCT, echography, cutometry test
Isotropy
Pre-tension
Anisotropic models

## Slide 19
prospects (2)
Estimate of the experimental stress field with Digital Image Correlation
Comparison with numerical results
Boundary conditions
Effect of dermis underneath the model
Study of sensibility
Tests on a phantom fabricated using a developed mold

## Slide 20
Thank you for your attention
Marco Sensale

## Slide 21
results and discussion (3)
Chart: Ogden 2° order
7.5 mm only keloid material | 0.0026791 | 0.0053455 | 0.0080006 | 0.010646 | 0.013282 | 0.015913 | 0.01854 | 0.021166 | 0.023795 | 0.026431 | 0.02908 | 0.03175 | 0.034447 | 0.037181 | 0.039965 | 0.042813 | 0.045741 | 0.048769 | 0.051921 | 0.055225 | 0.058714 | 0.062426 | 0.066408 | 0.070714 | 0.075412 | 0.08058 | 0.086316 | 0.092736 | 0.099984 | 0.10823 | 0.11769 | 0.12859 | 0.14125 | 0.15599 | 0.1732 | 0.19337 | 0.21701 | 0.24477 | 0.27737 | 0.31567 | 0.36072 | 0.41374 | 0.47621 | 0.54993 | 0.63708 | 0.7403 | 0.86285 | 1.0087 | 1.1826 | 1.3905
7.5 mm composite | 0.002711 | 0.0054111 | 0.0081016 | 0.010784 | 0.013459 | 0.016128 | 0.018795 | 0.021461 | 0.02413 | 0.026804 | 0.02949 | 0.032191 | 0.034915 | 0.03767 | 0.040465 | 0.043312 | 0.046225 | 0.049219 | 0.052314 | 0.055533 | 0.058904 | 0.062457 | 0.066231 | 0.070272 | 0.074633 | 0.079382 | 0.084597 | 0.090376 | 0.096835 | 0.10411 | 0.11238 | 0.12184 | 0.13272 | 0.14528 | 0.15983 | 0.17672 | 0.19635 | 0.21918 | 0.24574 | 0.27665 | 0.31264 | 0.35458 | 0.40352 | 0.46072 | 0.52772 | 0.60635 | 0.69888 | 0.80801 | 0.93698 | 1.0897